General:

KG-180 was developed to lower the cure temperature of Gun Kote (all bake on series) to address the need applicators had to coat substrates too sensitive to cure at 325F.

How it works:

KG-180 is a catalyst and when added to Gun-Kote starts “cross linking” the resins.  It does what “heat” does.

Instructions:

KG-180 could not be simpler to use.  2% of KG-180 added to the total material weight being sprayed is all that’s needed.  i.e. 1 ounce of Gun-Kote add .02 ounces of KG-180.  How to add ---- The cone tip on the bottle makes adding the KG-180 into your material easy, is accurate and takes the guess work out.  Simply cut the tip ½ inch from the top (1 inch from the bottom) and add 14 drops of 180 into every 1 once of material.  14 drops added to 1 ounce of material is equal to 2%.

Cure Temp after adding KG-180:    Can range from 170 to 185 for one hour.   Note:  To assure full cure perform a chemical (MEK/Acetone) rub test. You may see a little color coming off but you should not be able to take the coating off to bare metal.

The additive is forgiving but, adding more than recommended will ruin the coating.  The margin to work within is about +- 2 to 3 drops.  Less than the recommend 2% can be corrected by cure temp and time.

Adding amounts greater than 3% of the total material weight could destroy the coatings adhesion and chemical resistance.  Tests have been done at 4% and greater which resulted in catastrophic failure.

Caution:  The additive over time will cause Gun-Kote to gel and is the reason it should not be added back into the original can. The pot life is quite long for a catalyst however, >48 hours.

KG is continually testing the product.   As we learn more about it from customers and our own testing, we will provide updates when necessary.

Our Mission:	KG is committed to working with all companies, regardless of size.  We strive to provide Quality Products, Outstanding Customer Service and Technical support provided by experienced personnel.

# Text boxes

KG-180 Low Temp Additive

Revision 2017-2A