Although best known as a firearm finish KG Industries offers a full line of performance coatings and lubricants to Industrial and Commercial Applicators, Machine Shops, Engine Builders, Hand Built Bicycle Makers, OEM’s, Motorcycle Shops including Custom, Off Road and Street Bikes and high-end boat builders to apply at their own facilities.  Taking advantage of high performance coatings which, in the past, needed to be shipped at considerable costs is changing the relationship between the coating manufacturer and the end user which has opened new revenue streams to add to the bottom line.

Thin Film Coatings are a standard source for all types of performance gains by providing increased part protection, life span, durability, impact, corrosion and chemical resistance. The added capability to withstand harsh environments and applied in tight tolerances applications has made this technology a must for professionals looking for an extra edge.

Product Overview

Gun Kote 2400 Series

Gun Kote is a thin hard coating that will give excellent protection from abrasion.  It is not easily worn off like bluing, phosphate or chemically blackened surface treatments, which can leave metal surfaces, bare and unprotected from the elements. Gun Kote does not attract dirt or dust, has excellent impact resistance and can be formulated to meet specific customer’s needs.

Gun Kote 16/2 Flat Dark Earth was specified by the U.S. Military for special weapons in 2003. Gun Kote is now specified for 4 weapon systems and 500-pound 	bombs.

Gun Kote is formulated for lubrication using; molybdenum disulfide; PTFE or Boron.

Gun Kote is formulated for durability using a proprietary Melamine or Phenolic resin system and when Gun Kote is properly applied it will provide:

- Outstanding corrosion protection. Tests performed for Armscor by the South African Navel Logistics Dept. showed Gun Kote withstanding an equivalent of a 7-year exposure. (Tests were performed on Aluminum in a salt spray chamber with 50/50 on/off time at 35 degrees C.)

- Resistant to chemicals, oils and solvents common to Automotive, Aircraft, Motorcycles and Marine Industries.

- Helps to cool parts by dissipating heat.  Gun Kote will withstand temperatures over 500 degrees F and as low as -120 degrees F.

Gun Kote can be applied to all ferrous and non-ferrous metals, over all types of plating and some plastics.  Available in several colors including: Black, Gray, OD Green, Stainless Steel, Service Brown, Tan and the New Clear Kote.  Gun Kote's uses are only limited to the imagination! (Colors also available in Flat) Ask about our new 16/2 series High Gloss Black and Clear.  Premium Custom Colors also available in Greens, Blues, Pinks and Reds etc.

Page 2

Gun Kote and its uses:

- Exterior of weapons (including clips) of all types from handguns to G5 and G6 heavy artillery and bomb casings. The 500-pound bomb casings are specified to use KG)

- Engine blocks and heads to dissipate heat.

- Engine water jackets and water pumps.

- Protection from corrosion while helping to transfer heat and coolant.

- Transmission cases and rear end housings to transfer heat out. When used with Gear Kote and Engine Gard Oil Treatment will result in significant heat reduction.

- Radiators, oil and transmission coolers, to dissipate heat faster than bare metal while providing excellent corrosion protection.

- Brake Calipers, to provide heat dissipation, corrosion protection resulting in longer life.

These are just some of the applications of Gun Kote.  You are limited only by your imagination!

1200 Series Air Cure

KG’s New One Part Air Cured coating is a single component, water based, modified proprietary polyurethane resin system.  The 1200 Series is a fast curing system, formulated to compete and replace two-part water based coatings being marketed to various industries.

The 1200 has excellent adhesion, hardness, and flexibility. It is especially good for solvent sensitive substrates and for low VOC applications where a barrier coating is required.  The 1200 bonds extremely well to an array of substrates, metal, plastic and rubber but most impressive is substrates may not have to be profiled to assure adhesion.

The 1200  can be used for but is not limited to:

Outdoor Play Equipment

Protective Top Coatings for Camo Films

Wood or Synthetic Stocks for Firearms

Rubber hand Grips

Gear Kote 3000 Series

Gear Kote is a solid thin film lubricant, also known as dry film lubricant.  Gear Kote will provide a thin/lubricate film that will prevent galling and seizing.  Gear Kote aids in heat dissipation and protects the base metal from corrosion while reducing friction.  The appearance of Gear Kote is charcoal gray and upon burnishing will take on a sheen.  The ingredients of Gear Kote are solid lubricants and resin binders which provide the means to secure the lubricate solid to the base material.  The primary solid used for lubrication is Molybdenum Disulfide (MOs 2 or Moly) a lubricant known to withstand pressures in excess of 300,000 PSI.

In all applications, Gear Kote provides outstanding lubrication and corrosion protection for all major moving parts.  In firearm this would include slides, bolts and clips.  In Product automotive/motorcycle applications Gear Kote will provide reduced friction.  It will provide lubricity to gears, levers, cams, pistons and any sliding mechanism (Ball and Needle bearings excluded.) For industrial purposes, Gear Kote will provide an excellent dry film lubricant when combined with other coatings such as Tin or Titanium for use on drill bits. Gear Kote helps to reduce the operating temperatures of these components and will result in smoother pulls, rotation, actions and shifting.

Page 3

Gear Kote will provide:

- Outstanding corrosion protection for a dry lube. Gear Kote affords the user outstanding corrosion protection, a minimum of 100 hours salt spray at 5% salt.

- Resistant to chemicals, oils and solvents common to Aircraft, Industrial and Automotive Industries.

- Reduction of friction and heat. Gear Kote will withstand temperatures up to 500 degrees F and as low as -120F (Based on Cryogenic tests).

- Outstanding lubrication.

- Will not pick up dirt, dust or lint on exposed parts.

- Effective even if gearbox oil is lost.

Gear Kote can be applied to all ferrous and non-ferrous metals, over all types of plating and even some plastics.  Gear Kote's uses are only limited to the imagination!

Gear Kote Uses:

- Pistons, to eliminate friction and to provide better lubricity when used with oil.  Gear Kote is a very good heat distributor when used on pistons and domes.  This product will also shed carbon.  A combination of coated pistons and piston skirts will result in reduced damage from piston rock at bottom dead center.  Race engines have shown piston life improvement of over three times normal.

- Valve Spring and Retainers, to reduce guide wear.  Provide better distribution of heat on face of valves, and shed carbon. Improve air and fluid flow. Reduce wear and heat on springs, thereby increasing valve life and increases performance.

- Rod and Main Bearings, to provide a protective lubricant between mating parts. Always a lubricant in place.

- Crankshaft, Cams, Lifters, and Push Rods, to provide a protective lubricant in the event of momentary loss of oil and provide protective lubricant.

- Transmission and Rear End Gears, to reduce friction and gaining more power to the wheels.  Easier shifting and less wear on components.  Lighter weight oils can be used with protected parts leading to further performance gains.

- Gun and Rifle parts, to coat internal slides, trigger mechanisms leading to smoother pulls and permanent lubrication.

- Gearboxes of electric motors that drive conveyor lines resulting in fewer amps to drive motors which will result in less electricity used.

- Drill bits to reduce friction provide lubricity and increase production life.

- Trigger mechanisms, clip springs and pistol barrels for firearms.

- Marine Propellers to minimize cavitations.

C- Kote 6400 Series

Sold to professional applicators only, C-Kote is a true water reducible ceramic coating developed for the coating of exhaust manifolds, piston domes and other applications where high heat management and wear or abrasion resistance is required.  The 6400 Series will withstand continual temperatures of 1800F and intermittent spikes >2000F.

Page 4

Additional Products

KG is only one of two companies in the USA who produce both Moly and PTFE at sub-micron particle size.

Sub-Micron Suspended Moly, is an outstanding product used as an oil additive for gear boxes and internal combustion engines. It is also used to swab dies for hot stamping, and used to reduce bore fouling in the firearms industry.  If used in combination with Gear Kote it will provide the user many more benefits.  KG-6 will significantly reduce the friction and wear within engines and motors.

Sub-Micron Suspended PTFE.   Much like the Suspended Moly our sub-micron  PTFE (in oil) can be used as an additive for gear boxes and internal combustion engines.

Engine Gard, using our Suspended Moly, is one of the first moly oil additives that would not clog full flow oil filters.  Although considered older technology for an oil additive, Engine Gard is still a leading oil additive for race teams in both the automotive and motorcycle industries.

KG-3 Contact Cleaner, used for cleaning and decreasing parts.  KG-3 contains a special formulation of fast drying, water-displacing solvents, which rapidly cuts through oil and grease, leaving no residue. KG-3 is excellent for ignition points, plugs, and deep cleaning bearings and drive chains prior to lubrication, in all settings from Automotive to Industrial.

Assembly Lube, KG AD Paste is a molybdenum dry film lube developed to reduce wear, prevent galling and seizure of metals and provides corrosion protection. Used in the assembly of components AD will provide extra protection in start-ups. AD can also be used to touch up KG Gear Kote.

KG WL is a water based environmentally friendly solid film lube developed for the forging and swaging industry.  Formulated with Graphite and MoS2, KG WL will provide outstanding lubrication under extreme heat and pressure.  KG WL has been used at temperatures of up to 2300 degrees F with excellent results.

Industrial Uses

All KG products can be used for industrial purposes.  One leading manufacturer of tea uses the and Chain Kote.  They pour the Engine Gard into the gearboxes of the motors that drive the conveyer production lines, and spray the chains that drive the production lines with Chain Kote.  This same company tested these products over a four-year period.  They had bought 6 new, 1.2 million-dollar machines for their production facility.  Two of these machines were started with Chain Kote and Engine Gard.  The other four machines were started using the manufacturer’s recommendations.  After four years, the two machines with KG incurred approximately half the down time as the other four machines.

For maximum performance gains, combinations of the coatings with additives can be used.  For example, this company could have coated the gears with Gear Kote and experienced further performance gains.

All of the products mentioned have been tested over several years using racing teams, Dino’s, and have been subjected to rigorous testing in aerospace and military units.  In every case performance gains and or maintenance cost reductions were experienced. It is not unusual to have electric motors use less electricity, internal combustion engines gain RPM, sporting goods equipment to look better function better and last longer.

Page 5

Industrial Uses:

- Gear boxes to coat and or add Engine Gard into.

- Conveyor lines as a Chain Lube.

- Any and all chains found in the industrial setting.

- Any and all gearing that do not use clutches found in the industrial setting.

Other, More Exotic Uses for Our Coatings:

A combination of products such as Gear Kote and Gun Kote will provide outstanding results in high performance engines.  In recent tests, the intake manifold of a high output engine was coated with Gear Kote and the outside of the intake manifold was coated with Gun Kote.  This combination according to the builder resulted in a measured 5% increase in horsepower (20 horses) on Dyno.

Gun Care Products

Contrary to what some manufactures would have you believe, there is no one product on the market that will do what needs to be done to keep your firearms clean and safe.  Most important, none of our gun cleaning products contain ammonia.  KG has developed a system for cleaning that first addresses the removal of carbon from the bore with KG-1.  KG-2 or KG-12 then is used to remove the copper and lead fouling.  KG-3 is then used to remove the existing residue and KG-4 is then applied to protect the bore from the elements.

KG also produces a fine line of lubricants for the firearms Industry.  Included in this line is; KG-5 trigger lube; KG-6 Bore Prep; KG-7 Moly Powder; KG-8 Micro-PTFE Dry Lube, KG-9 Micro-PTFE Leather Kote, KG-10 Dry Lube, KG-11 Moly Grease, KG-112 Developed for the UK Special Forces and KG-410 Light Weight Penetrating Oil.

Oil Absorbent Matting:

The Bench Mat is a unique alternative to using news paper or towels to protect counter tops.  KG's Bench Mat protects work areas from messy and sometimes damaging oil and fluid spills.

Made from a non-woven polypropylene fiber the Bench Mat attracts and absorbs hydrocarbons preventing oils or solvents from damaging the work bench counter top. Making the Bench Mat even better is a non-slip backing.

The Bench Mat can be used in the Automotive, Motorcycle, Firearm, Machine Shops, Aircraft and many other industries.  The bench Mat also makes for an outstanding toolbox liner.

Visit our Web Site

www.kgcoatings.com

# Text boxes

KG Industries, LLC

204 Mustang Cove, Mustang Creek Industrial Park

Taylor, TX 76574

Phone:   (512) 352-3245   Fax:  (512) 352-3308

Information:  sales@kgcoatings.com

General Information